Hydrogen in indium oxide and gallium oxide

Chris G. Van de Walle

Materials Department, University of California, Santa Barbara, California, USA

Indium oxide, with a band gap of 2.7 eV, is widely used as a transparent conducting oxide. Gallium oxide, with a band gap of 4.8 eV, is also conductive and remains transparent into the UV, and (AlxGa1-x)2O3 alloys have even larger band gaps. Hydrogen is often introduced during growth or processing of the material; in fact, in the widely used technique of metal-organic chemical vapor deposition (MOCVD) hydrogen is present in the metal-organic precursors and often used as a carrier gas. It is therefore important to assess the impact of hydrogen on the properties of these materials. We address these issues using first-principles calculations based on density functional theory. In both In2O3[1] and Ga2O3[2] hydrogen acts as a shallow donor, i.e., it contributes to n-type conductivity, but its behavior changes in (AlxGa1-x)2O3 alloys.[3] Hydrogen can also interact with other impurities or defects in the material.

We have also studied diffusion. In monoclinic b-Ga2O3, the most stable phase, hydrogen diffusion is highly anisotropic.  For protons, the migration barrier is as low as 0.28 eV along the [010] direction.[3] In In2O3, with the bixbyite structure, local hopping of the proton, corresponding to a realignment of the O-H bond, can also occur with a low activation energy of 0.24 eV; however, this process does not lead to long-range diffusion.[4] The long-range migration path of H+ in In2O3 can be decomposed into rotations of the proton around oxygen and jumps between two oxygen atoms, with a higher overall activation energy of 0.94 eV. We compare our results with recent experiments.

Work performed in collaboration with M. L. D. Franckel, J. L. Lyons, S. Mu, M. E. Turiansky, J. B. Varley, D. Waldhör, M. Wang, and D. Wickramaratne.

[1] S. Limpijumnong, P. Reunchan, A. Janotti, and C. G. Van de Walle, Phys. Rev. B 80, 193202 (2009).

[2] J. B. Varley, J. R. Weber, A. Janotti, and C. G. Van de Walle, Appl. Phys. Lett. 97, 142106 (2010).

[3] S. Mu, M. Wang, J. B Varley, J. L Lyons, D. Wickramaratne, and C. G. Van de Walle, Phys. Rev. B 105, 155201 (2022).

[4] M. L. D. Franckel, M. E. Turiansky, D. Waldhör, and C. G. Van de Walle, Phys. Rev. B 110, L220101 (2024).