Ambient-Stable p-Type Transparent CuI Thin-Film Transistors via Room-Temperature Pulsed Laser Deposition

Yang Chen1, Michael S. Bar1, Susanne Selle2, Daniel Splith1, Michael Lorenz1, Marius Grundmann1, and Holger v. Wenckstern1.

1 Felix Bloch Institute for Solid State Physics, Faculty of Physics and Earth Sciences, Universität Leipzig, 04103 Leipzig, Germany.

2 Fraunhofer Institute for Microstructure of Materials and Systems IMWS, 06120 Halle, Germany。

As the first discovered p-type transparent conductive material, copper(I) iodide (CuI) is considered to be among the most competitive p-type candidates in the field of transparent electronics.[1] However, the strong compensation effect and air contamination lead to uncontrollable electrical properties.[2,3] As one of the most crucial transparent devices, CuI thin-film transistors (TFTs) face the critical challenge of balancing high performance and environmental stability. Herein, we propose a room-temperature pulsed laser deposition (PLD) process for ambient-stable, high-performance p-type CuI TFTs and circuits. By introducing a buffer layer  between 𝛾-CuI film and substrates, the CuI layer exhibits extremely low surface roughness (RMS < 1 nm), and the film thickness can be precisely controlled lower than 5 nm by the number of laser pulses. The free hole carrier concentration can be tuned from 1014 cm-3 to 1019 cm-3 and mobility can reach 25 cm2 V−1 s −1 comparable to that of bulk CuI by controlling the compensation effect from iodine deficiency.[4,5] In addition, a 200-nm-thick amorphous Al2O3 capping layer was deposited in situ on the thin CuI film. The concentration of free hole carriers in the covered film decreased by several orders of magnitude and remained stable in the air, enabling long-term device operation under ambient conditions. The optimized TFTs exhibit a field-effect mobility of over 0.5 cm2 V-1 s-1 and a high on/off current ratio of ~104 with good operational stability and reproducibility. This study provides a promising pathway toward ambient-stable transparent p-type field-effect transistors for complementary electronics in combination with n-type metal-oxide devices.

Reference

- Grundmann, Marius, et al. "Cuprous iodide–ap‐type transparent semiconductor: History and novel applications." physica status solidi (a) 210.9 (2013): 1671-1703.

- Storm, P., et al. "High mobility, highly transparent, smooth, p-type CuI thin films grown by pulsed laser deposition." APL materials 8.9 (2020).

- Liu, Ao, et al. "High-performance p-channel transistors with transparent Zn doped-CuI." Nature communications 11.1 (2020): 4309.

- Chen, Yang, et al. "Low-temperature buffer layer-assisted heteroepitaxial growth of γ-CuI thin films by pulsed laser deposition: Tailoring electrical properties." Applied Physics Letters 126.4 (2025).

- Bar, Michael S., et al. "Deconvolution of light-and heavy-hole contributions to measurements of the temperature-dependent Hall effect in zincblende copper iodide." Physical Review Applied 22.4 (2024): 044027.