Two-Layer ITO Metallization in Transparent Electronics

D. S. Memikoglu1, M. Ekström2, P. E. Hellström3,

1,2,3 KTH Royal Institute of Technology, Stockholm, Sweden

Introduction

Enabling invisible electronics requires that both transistors and interconnects are transparent in the visible spectrum [1]. Interconnects made of ITO offer >80% transparency in the visible range and a resistivity of ~100 μΩcm [2]. Currently, ITO is used as large-area electrodes, e.g., in solar cells, and typically patterned by wet etching. For metal pitch <10 µm, typically found in integrated circuits, dry etching is required. This study presents several key processes for implementing a two-layer ITO metallization scheme within a CMOS platform, with a focus on dry etching of ITO. These processes provide a way of fabricating transparent circuits.

Experiments & Results

ITO was deposited on thermally oxidized 100 mm silicon wafers with dc magnetron sputtering. Forming gas anneal (FGA) of ITO at 450 °C yielded sheet resistance of ~5 Ω/sq (400 nm).  ITO is patterned with I-line stepper lithography. An ICP-RIE process with CH4/Cl2/H2 chemistry and SiO2 hard mask was developed, enabling well-defined ITO layers with a 4 µm metal pitch (Tab. 1). The two-layer ITO metallization was evaluated with contact chain structures. I-V measurements across 120 chips demonstrated average contact resistance of ~85 Ω (Fig. 1). The compatibility of TiW/Al or TiN/Al to ITO was evaluated for the fabrication of measurement pads to provide external connections. While the measured resistance between TiW/Al and ITO was low (~3-5 Ω), metal delamination was observed in SEM after FGA (Fig. 2). TiN/Al on ITO was intact after FGA, albeit with higher resistance (~6-8 Ω).

Conclusions

A process to define 2 µm half-pitch ITO interconnects using dry etching has been established. Two-level metallization was evaluated by contact chains. The compatibility of TiW/Al and TiN/Al to ITO layer was investigated.

| Table 1. ICP-RIE details of ITO etch | (a) (b) Figure 1. (a) Schematic illustration of ITO to ITO contact experiment. (b) ITO to ITO contact resistance for 120 chips (RAVG = 85 Ω) |
| --- | --- |
| (a) (b) (c) (d) Figure 2. (a) Schematic illustration of TiW/Al or TiN/Al to ITO wafers. I-V results of (b) TiN/Al to ITO contact (c) TiW/Al to ITO contact. (d) Metal delamination of TiW/Al in SEM, the metal film burst from probing. |  |
| References [1] G. Thomas, Nature, vol. 389, pp. 907-908, 1997. [2] K. Ellmer, Nat. Photonics, vol. 6, pp. 809-817, 2012 | Acknowlegments This work was partly funded by Vinnova through Advanced Chip Technologies (grant 2023-00543), Swedish Foundation for Strategic Research (SSF RIF 2) and myfab. |